Enhanced structure stability, visible-light responsiveness and metallization in layered rhenium disulphide by pressure-induced phase transition

Pei Wang*,1,2,▼, Yonggang Wang1, 3, ▼ , Jingyu Qu1, 4, ▼, Qiang Zhu1, Liping Wang*, 1,  Dong Li2, Wenge Yang3, Jinlong Zhu1, Ligang Bai3, Weiwei Zhang4, Duanwei He2, and Yusheng Zhao*,1

1High Pressure Science and Engineering Center, University of Nevada, Las Vegas, Nevada 89154, United States

2Institute of Atomic and Molecular Physics, Sichuan University, Chengdu 610065, China

3High Pressure Synergetic Consortium (HPSynC), Geophysical Laboratory, Carnegie Institution of Washington, Argonne, Illinois 60439, United States

4Department of Applied Physics, China Agricultural University, Beijing 100080, China

Abstract: Rhenium disulphide with lower crystal symmetry in comparison with others transition metal disulphides, monolayers held together by weak forces semiconductor material, is a promising candidate for post-silicon electronics because of its unique optic-electronic properties. Pressure as an effective means is capable of continuous modulating its mechanical effects on the structural and electronic properties. The electrical and optical properties of rhenium dichalcogenide, however, remained unclear due to its low lattice symmetry. Here we present an experimental and theoretical study on the pressure-dependent structure, electronic, vibrational properties and visible-light responsiveness of rhenium disulphide up to 50 GPa. Our experimental results reveal that ReS2 undergo a phase transition at ~7.7 GPa followed by a sluggish semiconductor-metal transition at ~38.5 GPa, which is conﬁrmed by ab-initio calculations. The metallization arises from the overlap of the valance and conduction bands as a result of sulphur–sulphur interlayers sliding as the interlayer spacing reduces. Photocurrent measurements also indicate substantial enhancement in visible-light responsiveness of the layered ReS2 after high pressure treatments. The electronic transition affords modulation of the opto-electronic gain in rhenium disulphide.

Key words: High pressure, rhenium disulphides, metallization, visible-light responsiveness, and First-principles calculations

Introduction

Transition-metal dichalcogenides (TMDs) (MX2, where M denotes Mo, W, Re, and etc, X denotes S, Se and Te) have attracted tremendous interest because of their rich physics and unique opto-electronic properties.1-6 Layered TMDs held together with van der Waals (vdW) forces are a new class of quasi two-dimensional (2D) materials beyond graphene.1-7 Atomically thin monolayer TMD prepared by mechanical exfoliation or chemical vapour transports bond with strong covalent bonds within a X-M-X trilayer in its crystal structure, has been gradually explored to exhibit a wide range of electronic structures and exotic transport properties results from the various electron conﬁgurations of transition metals, such as quantum spin Hall effect (QSH),8 charge density waves (CDW)9-11 and superconductivity.12-14 As a family member of TMDs, rhenium disulphide (ReS2), is significantly different from others layer TMDs, it crystallizes in a layered structure is composed of a two hexagonal planes of S atoms and an intercalated hexagonal plane of Re atoms bound with S atoms forming chains of parallelogram-shaped Re4 clusters, which adopts a unique distorted-1T with lower lattice symmetry and weaker interlayer coupling than that of other TMDs under ambient condition.15-20 Unlike most of TMDs, Peierls distortion of the 1T structure of ReS2 with weakening the coupling interaction hinders S-Re-S layers from stacking ordered and minimizes the interlayer overlap of wave-functions.15-20 Because of that, ReS2 holds a bandgap semiconductor ~1.40 eV without transition from an indirect-bandgap bulk semiconductor to a direct-bandgap monolayer semiconductor,15-20 which is ideal for optics applications in the visible frequency range. The lack of high lattice symmetry, electronically and vibrationally decoupled in ReS2 gives rise to interesting anisotropic properties of both scientiﬁc and technologic importance, which opens opportunities for the development of pressure switches, logic circuits, sensors, and amplifiers with coupled electrical, vibrational, optical and structural properties using multilayered ReS2.15-22

High-pressure as a powerful means could efficient tune physical properties of materials via inducing lattice structures and electronic structures collapse.23-28 Such as layered MoS2 material has undergone a series of fantastic variable physical properties via continuous pressure modulating its crystal and electronic structures. Nayak et al. caught sight of a structural lattice distortion of layered MoS2 followed by an electronic transition from a semiconducting to metallic state at ~19 GPa.25 Moreover, pressure is able to control the band structure and optoelectronic properties of monolayer MoS2. Bandaru et al. showed a pressure-induced MoS2 isostructural hexagonal distortion to a 2Ha-hexagonal P63/mmc phase around 26 GPa.28 Subsequently, Chi et al. reported the appearance of metallization and superconductivity in pristine 2H-MoS2 at 90 GPa,23 the superconductivity transition temperature Tc(onset) reach up to 11.5 K under substantial compression.14 Zhao et al. also found MoSe2 possesses highly tunable transport properties under pressure owing to the gradual narrowing of band-gap followed by metallization.24 Nayak et al. discovered WS2 undergoes an isostructural semiconductor-to-metallic (S-M) transition at approximately 22 GPa at 280 K.26 Duwal et al. explored isostructural transition of WS2 driven by the presence of strong shear stress occurs displacively over a large pressure range between 15 and 45 GPa under nonhydrostatic compression.27 Recently, Guo et al. have experimentally realized metallization of layered VS2 would occur along with the compression of the vdW bonds.29

Unlike multilayered TMDs with high-symmetry crystal structures, the distorted-1T composition of multilayered ReS2 coupled with its d-orbital electronic states and the smaller 6.4 Å vdW interlayer gap increase the possibility of interlayer sliding under axial compression which might induce an electronic phase transition.15-20 Researches on ReS2 have been mainly focused on its opto-electronic properties of monolayers at ambient condition. Experimentally, few researches on ReS2 have been rarely studied its evolution of structures, opto-electronic responsiveness under high-pressure because of its complicated crystal structures. However, lattice structure and symmetry plays a key role in determining their fundamental properties. Hou et al. consider that ReS2 undergo a phase transition at about 10.5 GPa.30 Unfortunately, gradually broadening and merging together of diffraction lines in x-ray diffraction (XRD) patterns of ReS2 as a result of non-hydrostatic stress efficient lead to lack in further understanding of its high-pressure crystal structure. Furthermore, recent theoretical investigations have revealed that multilayered ReS2 will undergo a structural transition with a sluggish semiconducting to metallic (S–M) transition at continuous compression.20 However, it seems that the main peaks predicted by theoretical calculation are hard to match well with experimental XRD patterns. More experiments need to be performed to understand the structure evolution of ReS2 at high-pressure. More interesting, based on recent photoluminescence (PL) spectrum and reﬂectance spectrum experiments at ambient conditions indicated that multilayer ReS2 possesses an indirect optical gap at 1.40 eV,31 which is different from previous reported experimental and theoretical calculation results.15-22 This result has also been verified by Yan et al.32 The most promising and practical opto-electronic properties of ReS2 have also remained unexplored under high-pressure. Whether there are some links of the evolution of the crystal structure and electronic structure to possible metallization is still unclear. Therefore, there is lacking in deep understanding the experimental crystal structure, correlation of crystal-structure, S-M transition and visible-light responsiveness.

In this paper, combining with in-situ synchrotron x-ray diffraction (XRD), Raman scatting, electrical transport, visible-light-responds measurements and ab-initio calculations, we have systemically investigated crystal structures, metallization, vibrational response and photocurrents of ReS2 at pressures up to 50 GPa. The new high-pressure ReS2 phase has been successful predicted from ab-initio calculation and are good in agreement with experimental XRD data. XRD and Raman spectrum data reveal that ReS2 undergo a distorted-1T to distorted-1T′ phase transition at ~7.7 GPa and accompanied with hysteretic pressure-driven S-M transition at ~38.5 GPa, which are attributed to pressure-induced S···S interlayers sliding of ReS2 and finally result in changes in crystal structure and electronic structure. Improved structural stability also enhanced photo responsiveness for ReS2 via a pressure-induced phase transition.

Results

Structure details, synchrotron XRD patterns and volume dependence on pressure. ReS2 adopts a distorted CdCl2-type structure with low triclinic symmetry and a space group of P-1 at ambient conditions.33, 34 As shown in Fig. S1, each Re atom surrounded by six S atoms forms irregular [ReS6] octahedrons, which are edge – sharing and form ReS2 monolayer perpendicular to a-axis, Re atoms dimerizing each other form the chains denoted by the red zigzag line of parallelogram-shaped Re4 clusters because of the Peierls distortion (Figure S1 and S2), which appear throughout the single layer. Rhenium-sulfur (Re-S) bonds in ReS2 exhibiting diverse coordination environments are signiﬁcantly different from the case in MoS2, their lengths do not equal each other as shown in the Fig. S1. Figure 1a show the cross-section illustration of multilayered distorted-1T ReS2. One unit-cell only contains one S-Re-S sandwich. This stacking mode is known as distored-1T ReS2. Figure 1b shows the high-pressure experiment set up in DAC. The new high-pressure phase (called distorted-1T′) taking the same space group of P-1 as distorted-1T ReS2 has been predicted using USPEX approach. All Re atoms in new distorted-1T′ phase sharing the same (x, y) coordinate forming different S-Re-S triple layer packing is shown in the Fig. 1c. In order to minimize the interlayer S···S repulsion, the angles between triple layer distorted-1T′ phase change more contorted than distorted-1T phase, as shown in Fig. 1c. Upon compression to 8.9 GPa, all the peaks shift to larger two theta (smaller d-spacing), the (200) peak representing the interlayer spacing move fast to smaller d-spacing along the a-axis direction and merge into the trimer of (022), (120) and (002) peaks at 8.9 GPa (022) and (002) on the left and right of (120), repectively.). The trimer itself merges together, forming a single broad feature under high pressures. The rapidly pressure shift of (200) suggests that the a-axis is even more compressible than the b-axis and c-axis owning to decoupling interactions along the a-axis (Figure S3a). Under consecutive compression to 42.4 GPa, a new peak (marked using inverted-triangle) drills out as a left shoulder of the (220) peak beyond 8.9 GPa. The new phase was defined as distorted-1T′ which adopts the same space group of P-1 as that of distorted-1T phase. The crystal-structure of distorted-1T′ ReS2 was refined after predicting by theoretical calculations at 20 GPa (see Table S1). By fitting the volume as a function of pressure data to a third-order Birch-Murnaghan equation of state (BM-EoS) as shown in Fig. 1e,35 bulk modulus acquired is B0 = 35.6 ± 5.2 GPa with B0 = 10.8 ± 2.4 and V0 = 219.49 ± 0.81 Å3 for distorted-1T phase, and B0 = 49 ± 10 GPa with B0 = 5.4 ± 0.7 and V0 = 218.83 ± 3.65 Å3 for distorted-1T′ phase, respectively. Bulk modulus values of distorted-1T ReS2 agree well with the result of ref. 12: B0 = 23 ± 4 GPa with B0 = 29 ± 8.30 The pressure-dependent structure transition is anisotropic in Figure S3a and S3b in accordance lattice parameters and angles compression curve. The a-axis along layer direction is more compressible than b-axis and c-axis owing to weaker interlayer coupling forces. It is worth mentioning that the sulfur atoms in two adjacent hexagonal prismatic sheets are wiggled along the c-axis, minimizing the interlayer S···S repulsive forces in the distorted-1T′ structure.

Raman spectra, calculated bonds lengths and ELF results of ReS2 under high-pressure. The Raman spectroscopy reveals that up to 18 vibrational modes for ReS2 were observed due to its low lattice symmetry,15-18 which is obviously more than for TMDs with higher crystal symmetries, as shown in the Fig. 2a. Figure 2b shows that Raman active modes are quietly undergoing subtle change under compression, the feature of Ag-like mode corresponding to the out-of-plane vibrational mode located at 438 cm-1 S vibrations (a surface mode) along the a-axis (see Fig. 2b) is broadening and increasing above 9.4 GPa. Figure 2b shows the pressure-induced evolution in the most outstanding Raman peaks for bulk ReS2. The Raman peaks located at 153.1, 163.6, 217.2, and 237.2 cm-1  below 250 cm-1 basically come from Re vibration are less sensitive to hydrostatic pressure compared with others TMDs owing to ReS2 decoupled vibration, their pressure dependences of the vibrational frequencies approach to linear fitting, which indicates that nearly identical Re vibration in distorted-1T and distorted-1T′ phases. The sensitiveness of Cp located at 377.9 cm-1 and Ag-like located at 438 cm-1 differ from the former Eg-like modes, both of them exhibit phonon softening associated with the distorted-1T to distorted-1T′ phase transition in ReS2.15-18 We found that intensive vibration also occurs for Cp mode located at 377.9 cm-1 representing simplicity of in-plane and out-of-plane coupled mode of Re and S atoms also become magnified above 27.9 GPa. These distinct features above 250 cm-1 contributed basically by intensive S atoms motions account for experimental evidence for the presence of the distorted-1T′ phase because of the layer sliding and continuously increasing interlayer S···S interaction (Fig. 2c and 2d). 18, 23-27 Electron localization function (ELF) was calculated to further understand the physical origin of the interlayer S···S interaction for both phase ReS2 as shown in Fig. 2d-2f (Figure S4). The interlayer S-S distance decreases from 4.036 Å at ambient condition to 2.365 Å at 65 GPa, which indicates the formation of stronger interlayer S-S interaction beyond vdW forces (Fig. 2d).

Electric property measurements and the evolution of band gaps under high-pressure. To better understand the electronic behavior of ReS2 at high pressure, we performed in-situ resistance (R) measurements using quasi-four-point-probe methods in DAC and LVP (Figure S5 and S6). As shown in Fig. 3a-3d, the electrical resistance as a function of pressure and temperature (T). Upon compression, the resistance value decrease dramatically with increasing pressure, at least by 4 orders of magnitude, to a stable value of less than ∼1 Ω at ∼45.7 GPa, suggesting a semiconductor to metal transition, which is representatively owing to the broadening of the conduction and valence bands, induced by the shortening of chemical bonds.23-27 In-situ temperature-dependent resistance measurements (see Fig. 3b-3d) further corroborate the metallic behavior above 38.5 GPa. Resistance changes for bulk ReS2 imply the classical semiconducting behavior, as suggested by the negative temperature coefﬁcient of resistance value (dR/dT) at 12.3 GPa (Fig. 3b) for the semiconducting state. At 17.6 GPa, temperature-resistance curve reflects a semiconducting behavior similar to the ambient-pressure behavior at low temperature region, exhibiting positive dR/dT above 200 K indicating the presence of a typical metallic behavior.20, 23-27 The temperature-dependent resistance shows a positive dR/dT throughout all temperatures at 38.5 GPa, which is an indication of metallization of ReS2. The theoretical predicted transition result of closure of bandgap of ReS2 occur at ~40 GPa (Fig. 2f), which was theoretically found to associate with a vanishing band gap due to a S–M electronic transition.20, 23-27

Theoretical calculated band structure, angular momentum resolved density of states (LDOS) and charge density. The band structure and charge density of both distorted-1T and -1T′ ReS2 were also calculated using DFT theory with GGA method in order to further understand the origination of S-M transition under high-pressure (Figure S7). Recently experimental measurements of bandgap shown that ReS2 is an indirect-band-gap semiconductor with a band-gap of 1.40 at ambient condition.31 The band gap was regarded to reduce the binding energy of Re and S atoms in distorted-1T ReS2 in order to balance the increasing repulsion energy associated with Perils distortion, which result in forming of thermodynamic favorable ReS2 phase with low lattice symmetry. 15-17, 20, 23-27 To simplify the calculation, previous theory calculation show distorted-1T ReS2 is a direct-bandgap semiconductor via taking similar K-paths with hexagonal structure ReS2 (Figure S7). To figure out the band gap property of distorted-1T ReS2 at ambient condition, dense K-points were sampled in Brillouin zone. Figure 4a show that the cleavage bands in the valence band maxima (VBM) and conduction band maxima (CBM) locate at the different K point, which indicates that ReS2 is still an indirect-bandgap semiconductor with a bandgap is ~1.43 eV at ambient pressure. In order to obtain more information concerning the orbitals refer to the charge transfer. The angular momentum resolved density of states (LDOS) of distorted-1T phase at 0 GPa and distorted-1T′ phase at 42 GPa were also calculated to understand the contribution from the different orbitals of Re and S atoms (Figure 4b and 4c). Under compression of higher pressure, the band dispersions of conduction band and valence band get more crossovers due to the broadening of CBM and VBM (Figure S8). The Re dz2 orbital contributing to CBM increases, while the contribution from Re-p orbitals decreases.24, 25, 27 Likewise, the contribution to CBM reduces from S-px and S-py with the increase of pressure, while the contribution from S-pz increases.24, 25, 27 The charge density redistribution was also calculated to understand the effect of high-pressure in acquiring the S–M transition. As shown in Fig. 4d-4f, the charge density of S atoms increases with increasing pressure, which indicates the interlayer interaction is enhanced and induced the S-M transition.

Visible-light responsiveness measurements. In-situ photocurrent measurements of single-crystal and bulk semiconducting ReS2 samples were carried out under high-pressure in DAC. Visible-light harvesting ability for solar energy conversion applications is an important consideration for photovoltaic materials. 15, 17, 19, 21, 22, 37, 39  Both single-crystal and bulk ReS2 samples exhibit typical response to visible-light with on-off switch throughout all pressures, as shown in Fig. 5a and 5b. The photo responsiveness of ReS2 gradually enhance with the increasing pressure associated with the continuous decreasing the resistance value and band-gap under high-pressure (Figure 5c). Valence electrons are much easier to be excited by visible-light and get over barriers of bang-gap into CB due to the reducing bandgap with increasing pressure. Subsequently, photocurrent increases greatly because excitation photoelectron carriers start to migrate quickly and form closed-circuit. Bulk ReS2 is still be excited up to 39.3 GPa, which indicates its semimetal activity or that residual semiconducting samples were reserved due to heterogeneous nonhydrostatic condition in DAC. More interesting are the disappearing of photocurrent signals of single-crystal ReS2 at 27.8 GPa prior to that of bulk ReS2, which suggests that varying levels of sensitivity semiconductor-semimetal transition  are presumably attributed to the anisotropic conductivity of single-crystal ReS2 induced by its low lattice symmetry. The successive modulating of the electronic structure and band gap under irradiation of visible-light indicates possible energy-variable optoelectronics applications of ReS2 under controllable pressure.

In summary, we systematically investigated the structure evolution, electrical transport, vibrational properties and visible-light responsiveness of ReS2 under high-pressure up to 50 GPa combined with ab-initio calculations. In-situ high-P XRD and theoretical calculations results indicate that ReS2 undergo a phase transition at ~7.7 GPa followed by a semiconductor-metal transition at ~38.5 GPa. Raman spectrum, low temperature resistivity measurements, ELF and charge density calculation indicate that semiconductor-metal transition of ReS2 results from the overlap of the valance and conduction bands due to sulphur–sulphur interlayers sliding with the interlayer spacing reduces. Photocurrent measurements also suggest substantial enhancement in visible-light responsiveness of the layered ReS2 after high pressure treatments. The electronic transition affords modulation of the opto-electronic gain in ReS2.

Methods

In-Situ High-Pressure Characterizations. Powder and single-crystal ReS2 samples were purchased from Alfa Aesar and 2D Semicondcutors, respectively. High-pressure in-situ powder XRD experiments were carried out by use of a symmetric diamond anvil cell (DAC) with a culet size of 300 μm at 16-IDB of the High Pressure Collaborative Access Team (HPCAT), Advanced Photon Source (APS), Argonne National Laboratory (ANL) using a wavelength of 0.4066 Å with a 5 μm in diameter monochromatic X-ray beam. Powder ReS2 samples were loaded into a pre-indented rhenium gasket hole in diameter 170 μm for XRD and Raman spectroscopy experiments, while the pressure was determined using a ruby ﬂuorescence method and neon was used as the pressure-transmitting medium.36 XRD pattern were collected by a two-dimensional area PILATUS detector and integrated into one-dimensional proﬁle with the Fit2D program.37 Structure reﬁnements were performed using Pawley method.38 High-pressure electrical resistance (ER) evaluation was measured using a qusi-four-probe resistance measurement system consisting of a Keithley 6221 current source, a 2182A nanovoltmeter and 7001 voltage/current switch system and cubic large-volume press (LVP).39-41 Photocurrent measurements of powder and single-crystal samples were performed using an Autolab PGSTAT128N workstation which was used to keep track of the current-time (I-t) data.41 A 20 W incandescent lamp was chosen as the illumination source (∼2 W/cm2 on the sample). Dark current at μA level was produced by applying a constant voltage (varies from 0.002 to 0.3 V at a given pressure point depending on the ER. For example, 0.3 V at 4.7 GPa and 0.002 V at 39.3 GPa, respectively) owing to the changing of ER along the load pressure. 41

Theoretical Calculations. The search of high-pressure structures was carried out with variable-cell PSO35 structure prediction simulations using the evolutionary algorithm USPEX approach combining with Vienna ab-initio simulation package (VASP).42-44 All structures were locally optimized using the DFT method within the generalized gradient approximation (GGA) combining with VASP package.45 The all-electron projector augmented wave (PAW) method was adopted with a plane-wave kinetic energy cutoff of 500 eV for all calculations.46 For geometry optimizations and the band structure calculations of bulk ReS2, a set of 32×32×32 k-mesh samplings was employed for Brillouin zone integration. The convergence criterion of self-consistent field calculations for ionic relaxations was set for 10-5 eV for the totally energy. All unit cells and atomic positions were optimized until the atomic forces were less than ~0.01 eV/Å using the conjugate gradient method. Pressures on the lattice unit cell for the convergence criterion of relaxation were reduced to values 0.02 GPa and the Hellman-Feynman forces on the ions were less than 0.001 eV/Å.

References

- Wilson, J. A., Yoffe, A. D. The transition metal dichalcogenides discussion and interpretation of the observed optical, electrical and structural properties. Adv. Phys. 18, 193-335 (1969).

- Butler, S. Z. et al. Progress, challenges, and opportunities in two-dimensional materials beyond grapheme. ACS Nano 7, 2898-2926 (2013).

- Wang, Q. H. et al. Electronics and optoelectronics of two-dimensional transition metal dichalcogenides. Nat. Nanotechnol. 7, 699-712 (2012).

- Novoselov, K. S. et al. Two-dimensional atomic crystals. Proc. Natl. Acad. Sci. 102, 10451–10453 (2005).

- Radisavljevic, B. et al. Single-layer MoS2 transistors. Nat. Nanotechnol. 6, 147-150 (2011).

- Ferain, I., Colinge, C. A., Colinge, J. Multigate transistors as the future of classical metal-oxide-semiconductor field-effect transistors. Nature 479, 310–316 (2011).

- Geim, A. K., Novoselov, K. S.  The rise of grapheme. Nature Mater. 3, 183-191 (2007).

- Qian, X. et al. Quantum spin Hall effect in two-dimensional transition metal dichalcogenides. Science 346, 1344-1347 (2014).

- Calandra, M., Mauri, F. Charge-density wave and superconducting dome in TiSe2 from electron-phonon interaction. Phys. Rev. Lett. 106, 196406 (2011).

- Chatterjee, U. et al. Emergence of coherence in the charge-density wave state of 2H-NbSe2. Nat. Commun. 6, 6313 (2015).

- Shen, D. W. et al. Novel mechanism of a charge density wave in a transition metal dichalcogenide. Phys. Rev. Lett. 99, 216404 (2007).

- Suderow, H. et al. Pressure Induced Effects on the Fermi Surface of Superconducting 2 H− NbSe2. Phys. Rev. Lett. 95, 117006 (2005).

- Guillamón, I. et al. Superconducting density of states and vortex cores of 2H-NbS2. Phys. Rev. Lett. 101, 166407 (2008).

- Chi, Z. et al. Ultrahigh pressure superconductivity in molybdenum disulfide. ArXiv: 1503, 05331 (2015).

- Tongay, S. et al. Monolayer behaviour in bulk ReS2 due to electronic and vibrational decoupling. Nat. Commun. 5, 3252 (2014).

- Horzum, S. et al. Formation and stability of point defects in monolayer rhenium disulfide. Phys. Rev. B 89, 155433 (2014).

- Liu, E. et al. Integrated digital inverters based on two-dimensional anisotropic ReS2 field-effect transistors. Nat. Commun. 6, 6991 (2015).

- Feng, Y. et al. Raman vibrational spectra of bulk to monolayer ReS2 with lower symmetry. Phys. Rev. B 92, 054110 (2015).

- Ovchinnikov, D. et al. Disorder engineering and conductivity dome in ReS2 with electrolyte gating. Nat. Commun. 7, 12391 (2016).

- Zhou, D. et al. Pressure-induced metallization and superconducting phase in ReS2. NPJ Quantum Mater. 28, 19 (2017).

- Rahman, M. Davey, K. Qiao, S. Z. Advent of 2D Rhenium Disulfide (ReS2): Fundamentals to Applications. Adv. Funct. Mater. 27, 10 (2017).

- Zhang, Q. et al. Extremely Weak van der Waals Coupling in Vertical ReS2 Nanowalls for High‐Current‐Density Lithium‐Ion Batteries. Adv. Mater. 13, 2616-2623 (2016).

- Chi, Z. H. et al. Pressure-induced metallization of molybdenum disulfide. Phys. Rev. Lett. 113, 036802 (2014).

- Zhao, Z. et al. Pressure induced metallization with absence of structural transition in layered molybdenum diselenide. Nat. Commun. 6, 7312 (2015).

- Nayak, A. P. et al. Pressure-induced semiconducting to metallic transition in multilayered molybdenum disulphide. Nat. Commun. 5, 3731 (2014).

- Nayak, A. P. et al. Pressure-modulated conductivity, carrier density, and mobility of multilayered tungsten disulfide. ACS Nano 9, 9117-9123 (2015).

- Duwal, S., Yoo, C. S. Shear-induced isostructural phase transition and metallization of layered tungsten disulfide under nonhydrostatic compression. J. Phys. Chem. C 12, 5101-5107 (2016).

- Bandaru, N. et al. Effect of pressure and temperature on structural stability of MoS2. J. Phys. Chem. C 118, 3230-3235 (2014).

- Guo, Y. et al. Modulation of Metal and Insulator States in 2D Ferromagnetic VS2 by van der Waals Interaction Engineering. Adv. Mater. 29, 1700715 (2017).

- Hou, D. et al. High pressure X-ray diffraction study of ReS2. J. Phys. Chem. Solids 71, 1571-1575 (2010).

- Aslan, O. B. et al. Linearly polarized excitons in single-and few-layer ReS2 crystals. ACS Photonics. 3, 96-101 (2015).

- Yan, Y. et al. Associated Lattice and Electronic Structural Evolutions in Compressed Multilayer ReS2. J. Phys. Chem. Lett. 8, 3648-3655 (2017).

- Murray, H. H., Kelty, S. P., Chianelli, R. R., Day, C. S. Structure of rhenium disulfide. ‎Inorg. Chem. 33, 4418-4420 (1994).

- Lamfers, H. J., Meetsma, A., Wiegers, G. A., De Boer, J. L. The crystal structure of some rhenium and technetium dichalcogenides. J. Alloys Compd. 241, 34-39 (1996).

- Birch, F. Finite strain isotherm and velocities for single-crystal and polycrystalline NaCl at high pressures and 300 K. J. Geophys. Res. 83, 1257 (1978).

- Mao, H. K.; Xu, J.; Bell. M. Calibration of the ruby pressure gauge to 800 kbar under quasi-hydrostatic conditions. J. Geophys. Res. 91, 4673-4676 (1986).

- Hammersley, A. P. Two-dimensional detector software: from real detector to idealised image or two-theta scan. High Press. Res.14, 235–238 (1996).

- Pawley, G. S. Unit-cell refinement from powder diffraction scans. J. Appl. Crystallogr. 14, 357-361 (1981).

- Lü, X. et al.  Enhanced electron transport in Nb-doped TiO2 nanoparticles via pressure-induced phase transitions. J. Am. Chem. Soc.136, 419-426 (2014).

- Wang, P. et al. J. Diamond-c BN alloy: A universal cutting material. Appl. Phys. Lett.107, 037535 (2015).

- Wang, Y. et al. Pressure-induced phase transformation, reversible amorphization, and anomalous visible light response in organolead bromide perovskite. J. Am. Chem. Soc. 2015, 137, 11144-11149.

- Oganov, A. R., Glass, C. W. Crystal structure prediction using ab initio evolutionary techniques: Principles and applications. J. Chem. Phys.124, 244704 (2006).

- Zhu, Q. et al. Stability of xenon oxides at high pressures. Nature Chem. 5, .61-65 (2013).

- Kresse, G., Furthmuller, Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. J. Phys. Rev. B 54, 11169–11186 (1996).

- Perdew, J. P., Burke, K., Ernzerhof, M. Generalized gradient approximation made simple. Phys. Rev. Lett.78, 3865–3868 (1996).

- Blochl, P. E. Projector augmented-wave method. Phys. Rev. B 50, 17953–17979 (1994).

Acknowledgements

This work is supported by the National Nuclear Security Administration under the Stewardship Science Academic Alliances program through DOE Cooperative Agreement #DE-NA0001982. The use of HPCAT (16BM-B), APS is supported by the Carnegie Institute of Washington, Carnegie DOE Alliance Center, University of Nevada at Las Vegas, and Lawrence Livermore National Laboratory through funding from the DOE-National Nuclear Security Administration, the DOE-Basic Energy Sciences, and the NSF; the APS is supported by the DOE-BES, under Contract No. DE-AC02-06CH11357.

Author contributions

P.W., L.P.W., and Y.S.Z. designed the project. P.W. analyzed the data, and wrote the draft. Y.G.W and L.P.W. performed the synchrotron x-ray diffraction experiments. Y.G.W conducted Raman spectra, electrical resistance, and photocurrent measurements of ReS2 sample. D.L. performed electrical resistance measurements of ReS2 using LVP. J.Y.Q., Q.Z. and P.W. performed First-principles calculations. J.L.Z, L.G.B., and W.W.Z. co-wrote the paper. L.P.W, W.G.Y., D.W.H. and Y.S.Z edited the manuscript and also provided inputs for data interpretation. All authors discussed the results.

Supporting Information

Detailed sample characterizations (including crystal structure, band structure evolution of distorted-1T ReS2 under high-pressure, Pressure-dependence of lattice parameters and angles of layered ReS2 as a function of pressure, ELF, schematic of electrical resistance and electrical resistance measurements results using large volume press and PDOS at different pressures).

Additional information

Supplementary Information accompanies this paper at http://www.nature.com/naturecommunications

Competing financial interests: The authors declare no competing financial interests.

Figure captions

Figure 1. (Color online) Structure details, synchrotron XRD patterns and volume dependence on pressure of ReS2. (a) The cross-section illustration of layered distorted-1T ReS2. (b) Schematic diagram of the high-pressure diamond anvil cell (DAC) set up.  (c) The cross-section illustration of layered distorted-1T′ ReS2. (d) Selected XRD patterns of the ReS2 under high-pressure. Inverted-triangle indicates new diffraction peak from distorted 1T′ drill out. (f) The volume data of both phases of ReS2 as function of pressure fitted by 3rd order Birch-Murnaghan equation of state.

Figure 2. (Color online) Raman spectra results of ReS2 under high-pressure. (a) Raman spectra of ReS2 at room temperature and various pressures up to 50 GPa. The prominent modes Eg, Eg-like, Cp and Ag-like were indicated by arrows. (b) The evolution of the most prominent Raman peaks of ReS2 as a function of pressure. (c) The bond lengths dependence of ReS2 as a function of pressure. Insert shows the shortest S-S bond between interlayers. (d-f) The illustration of the key out-of-plane phonon mode Ag-like was shown in ELF profile.

Figure 3. (Color online) Electric property measurements and the evolution of band gaps of ReS2 under high-pressure. (a) Electrical resistance of ReS2 as a function of pressure at room temperature. (b-d) The temperature dependence of the resistance of ReS2 at 12.3, 17.6 and 38.5 GPa, respectively. (e) The calculated pressure-dependent band gap of layered ReS2. The first two data points calculated from distorted 1T phase, others from distorted 1T′ phase. The band gap closure is observed at 40 GPa. The bandgap dependence on pressure was fitted using a quadratic function, Eg = Eg + aP + bP2, where a = -51 meV GPa-1 and b = 0.47 meV GPa-2.

Figure 4. (Color online) Theoretical calculated band structure, angular momentum resolved density of states (LDOS) and charge density of ReS2. (b and c) Theoretical calculation of LDOS 0 GPa for distorted-1T phase and 42 GPa for distorted-1T′ phase. (d-f) Theoretical calculation of charge density of 0 GPa for distorted-1T phase and 14 and 65 GPa for distorted-1T′ phase, respectively.

Figure 5. (Color online) Photocurrent (a) of bulk ReS2 sample and (b) single-crystal ReS2 sample as a function of pressure. The sign of “on” and “off” represent visible-light source switch on and switch off, respectively. (c) Photocurrent—pressure dependence of bulk and single-crystal ReS2 samples.

Fig. 1

Fig. 2

Fig. 3

Fig. 4

Fig. 5

* Corresponding authors: pei.wang@unlv.edu, yushen.zhao@unlv.edu & liping.wang@unlv.edu ▼These authors contributed equally to this work. Correspondence and requests for materials should be addressed to P.W. (email:pei.wang@unlv.edu).